Reversible modification of magnetic properties of Fe3C nanoparticles by chemisorption of CO

N. A. Ivanova1, A. A. Onischuk1, S. V. Vosel1,3, P. A. Purtov1,

N. T. Vasenin2, V. F. Anufrienko2, V. N. Ikorski4

1Institute of Chemical Kinetics and Combustion SB RAS, 630090, Novosibirsk, Russia,

2Boreskov Institute of Catalysis SB RAS, 630090, Novosibirsk, Russia

3Institute of Geology and Mineralogy SB RAS, 630090, Novosibirsk, Russia

4International Tomography Center, SB RAS, 630090, Novosibirsk, Russia,

1. Introduction

The development of nanoscience and nanottechnology has resulted in various application of magnetic nanoparticles including magnetic targeting in drug delivery [1, 2], medical imaging [3, 4], gas sensing [5]. There is an enormous potential for the applications of nanoparticles in magnetic storage technology [6, 7]. The nano-size particles are of significant importance for the high-density magnetic recording [8 - 11]. If the medium density is to reach the value of 100 Gb/in2 or higher, the required magnetic grain size has to be about 10 nm or smaller [12]. The attractive properties of magnetic nanomaterials are enhanced coercivity [13] and magnetization [14 - 16] as well as superparamagnetism [17, 18] as the dimension approaches the nanoscale region. Magnetic nanoparticles embedded in nonmagnetic host materials, including carbon structures, are of interest because embedding provides encapsulation and prevents grain growth and agglomeration [19]. Fe3C nanoparticles have attracted a special attention due to the enhanced magnetic properties and diverse technological applications [20 - 27]. Important is that Fe3C particles are more resistant to oxidation than iron nanoparticles.

Generating microscopic magnetic patterns on the surfaces of nanoparticles is one of the goals of the modern nanotechnology development [28]. It is now well established that the particle magnetism can be changed essentially by the adsorption of gases [29-36]. The majority of the literature contributions on this subject is devoted to the chemisorption of H2, CO, O2 on Ni nanoparticles. It is shown that the adsorbed carbon monoxide reduces magnetic moments of Ni particles [30 - 33] due to the demagnetisation of individual atoms on Ni surface [28]. The adsorption of H2 and O2 on Ni surface may result in both decrease [30, 34] or increase [30, 35] of particle magnetisation. The adsorption of hydrogen on Fe clusters increases the magnetic moments of clusters substantially [36] and that of CO on cobalt clusters decreases the magnetization [29]. Unfortunately there is a lack of experimental data about the influence of gas adsorption on the magnetism of Fe3C nanoparticles.

The method of Electron Spin Resonance (ESR) is very sensitive to the properties of magnetic nanoparticles [37] especially to the modification of those by the gas adsorption [38]. That is why this techniques is widely used for the Fe3C magnetism investigation [20 - 22, 39, 40]

This paper is devoted to the ESR and magnetic measurements of Fe3C nanoparticles covered by a carbon structure. A special attention is paid to the changes of magnetic properties due to the particle interaction with CO and O2.

2. Experimental

The samples of Fe3C nanoparticles coated with carbon were prepared by co-pyrolysis of C3H8 + Fe(CO)5 diluted by Ar at atmospheric pressure. A flow quartz reactor (the inner diameter was 3.0 cm) with the outer resistive heating was used. The inlet molar fractions for propane and iron pentacarbonyl were, respectively, 6.0×10-2 and 1.8×10-5. The propane and iron pentacarbonyl decomposition degree were analysed by the gas-chromatography and IR spectrometry, respectively. The reactor operated at the inlet flow rate of 8 cm3s-1 (at STP) and temperature 1280 K which corresponded to the residence time 5.1 s and complete decomposition of C3H8 and Fe(CO)5. The pyrolysis resulted in aerosol particle formation which were sampled thermophoretically at the outlet of reactor to be analyzed by a Transmission Electron Microscope (TEM) JEM – 100SX and a High Resolution Transmission Electron Microscope (HRTEM) JEM – 2010. The phase composition studied by means of the X-ray diffraction (XRD) using a diffractometer URD-63 (CuK( radiation). The ESR measurements were carried out using X-band spectrometer Bruker ESP 300 at room temperature. The magnetic measurements were carried out by a vibration magnetometer SQUID MPMS XL (Quantum Design). XRD samples as well as samples for ESR and magnetic measurements were obtained collecting the aerosol particles by a high efficiency aerosol filter. In the case of ESR analysis the deposit was detached from the filter and put to a quartz test tube.

3. Results and discussion

A typical TEM images of particles sampled at the reactor outlet are shown in Fig. 1. The only phase observed by the XRD method was Fe3C (see Fig. 2). The high contrast regions (see insert in Fig. 1) are Fe3C particles, while the low contrast matter is carbon. One can see that there are small Fe3C nanoparticles (of size from a few to a few tens nanometer). In more detail the structure of sampled particles is shown in Fig. 3. There are graphite-like layers of carbon adjoining the Fe3C particles. However, the main part of carbon is amorphous.

Fig. 4 compares ESR and magnetic measurements data. The ESR spectrum from the as-prepared sample is demonstrated in Fig. 4a. One can see the line from carbon radical centers (g = ge) marked as “Carbon” and other broad lines which are related to the Fe3C phase. The ESR spectrum has changed essentially after the sample being treated by the water vapor (at T = 723 K, PH2O = 20 Torr, exposure time t = 1 hour) or CO (at T = 573 K, PCO = 4 Torr, t = 2 hours), see Figs. 4 b and c. Note, the water exposure at T = 723 K has resulted in the sample treatment by CO which was formed via the reaction H2O + C ( CO + H2. On the other hand, the CO exposure has resulted in the strong decrease of ferromagnetism of the sample (compare Figs 4e and f). The further air exposure of this sample during 10 days has restored the magnetization up to the initial value of 0.2 Gs cm3g-1 (see Fig. 4g), and the ESR spectrum has become about the same as the initial one (Figs. 4a and d).

Thus, there is no correlation between the ESR spectra and the specific magnetization curves. Therefore we assume that the ESR signals are not related directly with the ferromagnetism of Fe3C particles. On the other hand, the spectrum observed can not be attributed to the paramagnetic resonance from Fe0 or Fe2+ isolated ions, because these species have a very short relaxation time at the room temperature i.e. the line width is very broad to observe the ESR spectrum. The concentration of Fe3+ ions is negligible in the sample under consideration, because the sample was synthesized in a highly reducing medium. Therefore, we attribute the ESR signals to superparamagnetic Fe3C particles. The chemisorbed CO has demagnetized the surface layers of Fe3C particles resulting to the transition of some of Fe3C nanoparticles from ferromagnetic to superparamagnetic state and other particles from superparamagnetic to paramagnetic state. The following air exposure has removed CO from the surface and restored the magnetization.

TEM and HRTEM images (Figs. 1, 2) support the assumption that the ESR signals are caused by superparamagnetic Fe3C particles demonstrating the presence of small particles with the size of about 10 nm. The strong increase of the ESR spectrum intensity at low magnetic field (see. Fig. 4 a – d) also supports the assumption. As known this strong increase is typical for the superparamagnetic resonance [41] as in contrast to the ferromagnetic one. Besides, as seen from Fig. 4g the coercitivity is quite different from that of the initial sample (Fig. 4e); it can be explained by the superposition of the ferromagnetic and superparamagnetic states only. (Note, the coercitivity for the superparamagnetic state is equal to zero).

References

1. M. A. Morales, T. K. Lain, V. Labhasetwar, D. L. Leslie-Pelecky, Magnetic studies of iron oxide nanoparticles coated with oleic acid and Pluronic® block copolymer. Journal of Applied Physics, 2005, 97, 10Q905(1-3).

2. S. Yu, G. M. Chow, Carboxyl group (-CO2H) functionalized ferrimagnetic iron oxide nanoparticles for potential bio-applications. J. Mater. Chem., 2004, 14, 2781 – 2786.

3. M. A. Albrecht, C. W. Evans, C. L. Raston Green chemistry and the health implications of nanoparticles. Green. Chem. 2006, 8, 417 – 432.

4. H. Nishibiraki, C. S. Kuroda, M. Maeda, N. Matsushita, M. Abe, H. Handa, Preparation of medical magnetic nanobeads with ferrite particles encapsulated in a polyglycidyl methacrylate (GMA) for bioscreening. Journal of Applied Physics, 2005, 97, 10Q919(1-3).

5. A. Pinnoose, K. M. Reddy, J. Hays, A. Thurber, M. H, Engelhard, Magnetic gas sensing using a dilute magnetic semiconductor. Applied Physics Letter 2006, 89, 112509 (1-3).

6. T. Heyon, Chemical synthesis of magnetic nanoparticles. Chem. Commun. 2003, 927 - 934

7. S P Gubin, Yu A Koksharov, G B Khomutov, G Yu Yurkov, Magnetic nanoparticles: preparation, structure and properties. RUSS. CHEM. REV., 2005, 74(6), 489 – 520.

8. X. Q. Zhao, B. X. Liu, Y. Liang, Z. Q. Hu, Oxidation behaviour and magnetic properties of metallic ultrafine particles. Journal of magnetism and magnetic materials 164 (1996) 401 – 410

9. J. Hoinville, A. Bewick, D. Gleeson, R. Jones, O. Kazyutich, E. Mayes, A. Nartowski, B. Warne, J. Wiggins, K. Wong, High density magnetic recording on protein-derived nanoparticles. Journal of Applied Physics, 2003, 93(10), 7187 – 7189.

10. J.-M. Qiu, Y.-H. Xu, J. H. Judy, J.-P. Wang. Nanocluster deposition for high density magnetic recording tape media. Journal of Applied Physics, 2005, 97, 10P704(1-3).

11. J. A. Christodoulides, Y. Zhang, G. C. Hadjipanayis, C. Fountzoulas, CoPt and FePt nanoparticles for high density recording media. IEEE transactions on magnetics, 2000, 36(5), 2333 – 2335.

12. Y.H. Lee, T. C. Han, J.C.A. Huang, C. R. Lin, Analysis of microstructure of magnetic Fe3C nanograins embedded in carbon films. Journal of Applied Physics, 2003, 94(3), 1975 – 1978

13. G. L. Zhang, H. Pattyn, embedded nanocrystallites prepared by ion implantation. Hyperfine interactions, 1998, 113, 165 – 181.

14. X. Y. Li, L. T. Kong, B. X. Liu, Enhanced magnetic moment of Fe in fcc-structured Fe-Ag and Fe-Au alloys synthesized by ion-beam manipulation. Phys. Rev. B, 2005, 72, 054118 (1-6).

15. Y. Xie, J. A. Blackman, Magnetism of iron clusters embedded in cobalt. Phys. Rev. B, 2002, 66, 085410 (1-5).

16. S. Yu, G. M. Chou, Synthesis, structural, magnetic, and cytotoxic properties of iron oxide coated iron/iron-carbide nanocomposite particles. Journal of Applied Physics, 2005, 98, 114306 (1-7).

17 T. Enz, M. Winterer, B. Stahl, S. Bhattacharya, G. Miehe, K. Foster, C. Fasel, H. Hahn, Structure and magnetic properties of iron nanoparticles stabilized in carbon. Journal of Applied Physics, 2006, 99, 044306 (1-8).

18. M. E. McHenry, S. A. Majetch, J. O. Artman, M. DeGraef, S. W. Staley, Superparamagnetism in carbon coated Co particles produced by the Kratschmer carbon arc process. Phys. Rev. B, 1994, 49 (16), 11358 -11363.

19. F.S. Denes, S. Manolache, Y. C. Ma, V. Shamamian, B. Ravel, S. Prokes, Dense medium plasma synthesis of carbon/iron-based magnetic nanoparticle  system. Journal of Applied Physics, 2003, 94(5), 3498 – 3508.

20. U. Narkiewicz, W. Arabczuk, I. Pelech, N. Guskos, J. Typek, M. Maryniak, M. J. Wozniak, H. Matysiak, K. J. Kurzydlowski, Materials Science-Poland, 2006, 24(4), 1067 – 1075.

21. N. Guskos, J. Typek, M. Maryniak, U. Narkiewicz, I. Kucharewicz, R. Wrobel, FMR studies of agglomerated nanoparticles in a Fe3C/C system. Materials Science-Poland, 2005, 23(4), 1001 – 1008.

22. N. Guskos, E. A. Anognastakis, V. Likodimos, T. Bodziony, J. Typek, M. Maryniak, U. Narkiewicz, I. Kucharewicz, S. Waplak, Ferromagnetic resonance and ac concuctivity of a polymer composite of Fe3O4 and Fe3C nanoparticles dispersed in a graphite matrix. Journal of Applied Physics, 2005, 97, 024304 (1-6).

23. N. Guskos, J. Typek, M. Maryniak, U. Narkiewicz, W. Arabczuk, I. Kucharewicz, Temperature dependence of FMR spectrum of Fe3C magnetic agglomerates. Journal of Physics: Coference Series, 2005, 10, 151 – 154.

24. Y. H. Lee, T. C. Han, J. C. A. Huang, Magnetic properties of Fe3C nanograins embedded in carbon matrix. Journal of Applied Physics, 2003, 93(10), 8462 – 8464.

25. E. P. Sajitha, V. Prasad, S. V. Subramanyam, S. Eto, K. Takai, T. Enoki, Synthesis and Characteristics of Iron Nanoparticles in a Carbon Matrix Along with the Catalytic Graphitizationof Amorphous Carbon. CARBON 2004, 42(14), 2815-2820.

26. K. Lipert, J. Kazmierczak, I. Pelech, U. Narkiewicz, A. Slawska-Waniewska, H. K. Lachowicz, Magnetic properties of Cementite (Fe3C) Nanoparticle Agglomerates in a Carbon Matrix. Materials Science-Poland, 2007 in press.

27. E. P. Sajitha, V. Prasad, S, V. Subramanyam, A. K. Mishra, S. Sarkar, C. Bansal, Size-dependent magnetic properties of iron carbide nanoparticles embedded in a carbon matrix. journal of Physics: Condensed Matter, 2007, 19, 046214 (13 pp)

28. Q. Ge, S. J. Jenkins, D. A. King, Localisation of adsorbate-induced demagnetisation: CO chemisorbed on Ni {110}. Chem. Phys. Lett. 2000, 327, 125 – 130

29. F. Reboredo, G. Galli, Size and Structure Dependence of Carbon Monoxide Chemisorption on Cobalt Clusters. J. Chem. Phys. B, 2006, 110, 7979 – 7984.

30. M. B. Knickelbein, Nickel clusters: The influence of adsorbates on magnetic moments Chem. Phys. Letters. 2002, 116(22), 9703 - 9711

31. N. Cordente, C. Amiens, B. Chaudret, M. Respaud, F. Senocq, M.-J. Casanove, Chemisorption on Nickel Nanoparticles of Various Shape: Influence on Magnetism. Journal of Applied Physics, 2003, 94(10), 6358 – 6365.

32. C. S. Fergerie, A. Seiler, J. L. Pena, R. J. Celotta, D. T. Pierce, CO Chemisorption on Ni(110: Effect on Surface Magnetism. Phys. Rev. Letters 1986, 56(20), 2207 – 2210.

33. M. Knickelbein, Nickel Clusters: The influence of adsorbed CO on magnetic moments. Journal of Chemical Physics 2001, 115(5), 1983 – 1986.

34. F. Passek and M. Donath, Magnetic surface state becomes nonmagnetic by oxygen adsorption. Phys. Rev. Lett. 1993, 71(13), 2122 – 2125

35. L. Stradella, E. Genova, The influence of Chemisorbed gases on the magnetization of transition metals. Journal of Materials Science letters 1995, 14, 44 – 45.

36. M. B. Knickelbein, Adsorbate induced enhancement of the magnetic moments of iron clusters. Chem. Phys. Letters. 353 (2002) 221 – 225.

37. W. S. D. Folly, R. S. de Biasi, Determination of Particle Size Distribution by FMR Measurements. Brazillian Journal of Physica 2001, 31(3), 398 – 401.

38. A. A. Slinkin, Application of FMR for study of heterogeneous catalysts. RUSS. CHEM. REV., 1968, 37(8), 1521 – 1543.

39. M. Maryniak, N. Guskos, J. Typek, I. Kucharewicz,U. Narkiewicz, Z. Rozlaniec, ,M. Kwiatkowska, W. Arabczyk, K. Aidinis, FMR Study of polymer composites with nanocrystalline iron-carbom fillers. Rev. Adv. Mater. Sci. 2006, 12, 200 – 205.

40. N. Guskos, J. Typek, T. Bodziony, Z. Roslaniec, U. Narkiewicz, M. Kwiatkowska, M. Maryniak, Temperature Dependence of FMR Field of Magnetic Nanoparticles/Polymer Composite. Rev. Adv. Mater. Sci. 2006, 12, 133 – 138.

Figure Captions

Fig. 1. Typical TEM images of the samples used in magnetic and ESR measurements

Fig. 2. XRD spectrum from Fe3C phase being a constituent of samples formed by co-pyrolysis of C3H8 and Fe(CO)5 diluted by Ar.

Fig. 3. High Resolution TEM image of Fe3C – Carbon particles sampled at the reactor outlet.

Fig. 4. ESR spectra (a – d) and specific magnetization curves (e-g); a, e – as-prepared sample; b – treated by water vapor, c, f – treated by CO, d, g – exposed to the air during 10 days.

Fig. 1. Typical TEM images of the samples used in magnetic and ESR measurements

Fig. 2. XRD spectrum from Fe3C phase being a constituent of samples formed by co-pyrolysis of C3H8 and Fe(CO)5 diluted by Ar.

Fig. 3. High Resolution TEM image of Fe3C – Carbon particles sampled at the reactor outlet.

# Text boxes

g

e

f

a

b

c

d

Fig. 4. ESR spectra (a – d) and specific magnetization curves (e-g); a, e – as-prepared sample; b – treated by water vapor, c, f – treated by CO, d, g – exposed to the air during 10 days.